Firebreak Formula's

Version 1.0

Eight Mineral-Based, Environmentally Safe Firebreak and Fire Suppression Formulas

Improved Paths A through D, plus four new weather-resistant variants

| Document | Firebreak Formula's v1.0 |
| --- | --- |
| Status | Field formulation reference |
| Scope | Passive barriers, binders, slabs, aerial drops |
| Safety class | Environmentally safe mineral recipes |

# Table of Contents

Right-click the table and select "Update Field" to refresh page numbers.

1. Purpose and Scope	3

2. Design Principles	4

3. Materials Reference	5

4. Part One: The Four Improved Formulas	7

Formula 1: Emberline Base (Improved Path A)	7

Formula 2: Ashbinder Powder (Improved Path B)	9

Formula 3: Hearthstone Slab (Improved Path C)	11

Formula 4: Skyfall Blanket (Improved Path D)	13

5. Part Two: Four New Formulas	15

Formula 5: Stonegrain Pellets (Derived from Path A)	15

Formula 6: Clayshield Coating (Derived from Path B)	17

Formula 7: Hearthpaver Tiles (Derived from Path C)	19

Formula 8: Deepseal Grout (Derived from Path D)	21

6. Master Comparison Table	23

7. Environmental Safety Verification	24

8. Testing and Quality Control Protocols	26

9. Field Deployment Guide	28

10. Bulk Sourcing Guide	30

11. Naming Convention	31

# 1. Purpose and Scope

This document presents eight mineral-based formulas for wildfire defense: four improved versions of the original Path A, B, C, and D recipes, plus four new formulas derived from them. Every formula prioritizes two goals. First, each mix resists rain and wind, whether spread on the ground or dropped from aircraft. Second, every ingredient remains environmentally safe before, during, and after use.

All formulas draw on cheap, bulk materials: quarry waste, mine tailings, sawmill residue, common clay, agricultural lime, and plaster. No formula uses ammonium phosphate, borate compounds, PFAS chemistry, synthetic polymers, or any material with documented aquatic or soil toxicity.

Each formula carries a descriptive, politically neutral name alongside its original Path designation, so crews, engineers, and suppliers share one unambiguous vocabulary.

# 2. Design Principles

### 2.1 Rain and Wind Resistance

The original loose mixes failed in weather because light biochar particles floated away in rain and blew away in wind. The improved formulas solve this with physics rather than exotic chemistry:

- Angular crusher dust interlocks with quartz fines and physically traps biochar particles inside the mineral matrix.

- Sodium bentonite clay coats each particle and swells when wet, gluing the matrix together and forming a self-sealing surface crust.

- Pelletization (Formula 5) converts loose powder into dense granules that punch through smoke columns and resist wind drift during aerial drops.

- Light misting plus tamping activates surface tension between particles and raises bulk density, so raindrops strike a firm mat instead of loose sand.

### 2.2 Environmental Safety

Every ingredient passes a simple three-part test: it occurs in nature or derives directly from natural minerals, it leaves no persistent toxic residue, and post-fire residue benefits or at least does no harm to soil. Section 7 documents this verification ingredient by ingredient.

### 2.3 Accessibility and Cost

Every added ingredient comes from sources that sell it in bulk at low cost: quarries, sawmills, agricultural suppliers, hardware stores, and pottery or drilling suppliers. Section 10 lists typical sources and prices.

# 3. Materials Reference

The table below defines every material used across the eight formulas. Mass measurements, not volume, govern all recipes.

| Material | Specification | Role | Environmental Profile |
| --- | --- | --- | --- |
| Quartz tailings (silica fines) | Pass < 2 mm sieve, dry | Primary structure and heat sink | Inert mineral; mine waste diverted from containment ponds |
| Granite fines (whole rock) | Pass recipe sieve size | Supplies alumina, iron, and alkali oxides | Inert quarry waste; matches natural soil minerals |
| Crusher dust / quarry screenings | 0 to 5 mm, gap-graded, angular | Mechanical stabilizer; locks particles together | Inert quarry byproduct; identical to crushed road base |
| Biochar / wood ash (fully burned sawdust) | Pass < 1 mm sieve, volatile matter < 3% | Insulation and thermal buffering | Pure carbon and mineral ash; a recognized soil amendment |
| Sodium bentonite clay | Fine powder, no additives or fragrance | Swelling binder and oxygen sealant | Natural clay; used in pond liners, drilling mud, and food products |
| Hydrated lime Ca(OH)2 | Agricultural or builders grade | Alkaline activator and crust former | Standard agricultural soil amendment; carbonates back to limestone over time |
| Gypsum CaSO4 (plaster) | Hardware plaster or agricultural gypsum | Endothermic coolant; releases bound water near 150 C; accelerates set | Natural mineral; agricultural soil conditioner |
| Cornstarch | Food grade, bulk sack | Biodegradable binder for pellets and coatings | Food product; fully biodegradable |
| Molasses or brown sugar | Feed grade or food grade | Set retarder giving longer working time | Food product; fully biodegradable |
| Sodium silicate solution (water glass) | Optional activator, industrial grade | High-strength binder activator | Inert silica gel after cure; handle wet solution with gloves |
| Dry ice pellets (optional, Formula 8) | Food or industrial grade CO2 | Deep cooling and oxygen displacement | Sublimates to atmospheric CO2; zero residue |
| Iron oxide pigment (optional) | Natural iron oxide, red or buff | Visibility marker for aerial drops and coatings | Natural rust pigment; soil-safe |

Table 1: Materials used across all eight formulas.

Handling Safety (Distinct from Environmental Safety)

Crystalline silica dust harms lungs. Wear an N95 mask for dry mixing and a P100 respirator for fine milling.

Hydrated lime and wet sodium silicate burn skin and eyes. Wear gloves and goggles, and wash skin promptly after contact.

Biochar and wood ash run alkaline (pH near 10). Wear gloves.

Kiln work for Formula 2 runs at 650 to 750 C. Ventilate the workspace and follow standard furnace safety practice.

# 4. Part One: The Four Improved Formulas

Each formula below upgrades one original path. The improvements target one weakness above all: the mix stays in place through wind and rain instead of scattering or washing out.

## Formula 1: Emberline Base (Improved Path A)

A cheap, bulk, rapidly deployed thermal barrier for ground crews. This version adds crusher dust for mechanical interlock and bentonite clay for a self-sealing surface crust, so the barrier survives wind and repeated rain events.

| Attribute | Value |
| --- | --- |
| Role | Loose, weather-stabilized ground firebreak |
| Cost | About $0.06 to $0.10 per kg |
| Lifespan | One to two fire seasons, or five to eight heavy rain events |
| Rain tolerance | High for a loose material; bentonite crust self-seals after wetting |
| Wind tolerance | High; angular particles interlock and the clay binds the surface |

### Recipe (Makes 100 kg)

| Component | Mass | Sieve Size | Function |
| --- | --- | --- | --- |
| Quartz tailings (fines) | 50 kg | < 2 mm | Primary structure and heat sink |
| Crusher dust / quarry screenings | 15 kg | < 5 mm, gap-graded | Mechanical stabilizer; angular particles lock together |
| Biochar / wood ash | 27 kg | < 1 mm, volatile matter < 3% | Insulation and thermal buffering |
| Sodium bentonite clay | 8 kg | Fine powder | Swelling binder; forms a rain-resistant surface crust |

### Mixing Protocol

- Pre-dry the quartz, crusher dust, and biochar in the sun for 24 hours, or in an oven at 100 C for 2 hours. Moisture above 5% causes steam spalling under flame.

- Slake the bentonite: stir the 8 kg of clay into about 12 liters of water until it forms a thin slurry like pancake batter. Let it stand 30 minutes to fully hydrate.

- Coat the biochar first: toss the 27 kg of biochar into the clay slurry and mix until every particle carries a light clay film. This core-shell step preserves the insulation pores of the biochar.

- Add the 50 kg of quartz fines and 15 kg of crusher dust. Mix 7 to 10 minutes until the color turns uniform dark grey.

- Spread the mix to a minimum thickness of 12 cm and a minimum width of 2 meters.

- Tamp the surface with the back of a rake or a hand tamper until firm at roughly 70 to 75% density. A light water mist before tamping improves the bond.

- Let the barrier dry for 24 hours. The bentonite sets into a firm, erosion-resistant crust.

### Weather Behavior

- Wind up to 60 km/h: no visible erosion; the crust holds.

- Light rain under 10 mm: the bentonite swells and seals tighter; no material loss.

- Moderate rain of 10 to 30 mm: surface softens, then re-seals on drying; rake the top 2 cm after drying to restore texture.

- Heavy rain above 30 mm: the mat stays in place; re-test with the torch test after drying and top-dress with fresh biochar if the test fails.

### Deployment Checklist

☐ Torch test passes on a 500 g sample: no sustained glowing and no smoke after flame removal.

☐ Materials start bone-dry before mixing.

☐ Barrier runs continuous, 12 cm thick and 2 m wide, with no gaps.

☐ Surface stays clear of leaf litter and pine needles.

## Formula 2: Ashbinder Powder (Improved Path B)

A fine, reactive pozzolanic powder that mimics volcanic ash. The improved version ships as a self-activating blend: hydrated lime comes pre-mixed into the dry powder, so field crews add only water. The powder stores indefinitely in sealed bags, and the cured product sheds rain permanently.

| Attribute | Value |
| --- | --- |
| Role | Reactive binder for mortar, grout, slabs, pellets, and coatings |
| Cost | About $0.15 to $0.20 per kg (milling and heat treatment drive the cost) |
| Lifespan | Indefinite as dry powder; permanent once cured |
| Rain tolerance | Critical to protect during the 7-day cure; fully waterproof after 14 days |
| Wind tolerance | Not applicable as powder; the cured binder forms a solid ceramic-like mass |

### Recipe (Makes 100 kg of Self-Activating Binder)

| Component | Mass | Sieve Size | Function |
| --- | --- | --- | --- |
| Silica tailings (pure SiO2) | 57 kg | < 45 microns (325 mesh) | Bulk silica backbone |
| Granite fines (whole rock) | 38 kg | < 45 microns (325 mesh) | Alumina, iron, and alkalis; the volcanic ash oxide balance |
| Hydrated lime Ca(OH)2 | 5 kg | < 0.5 mm | Pre-blended alkaline activator; field crews add only water |

### Processing Protocol

- Crush oversized feedstock to below 5 mm with a jaw crusher or heavy hammer.

- Mill the silica and granite to 100% passing a 325-mesh (45-micron) sieve. Coarser particles react too slowly to serve as a pozzolan.

- Dry-blend the 57 kg of silica and 38 kg of granite for 10 minutes until the powder shows no streaks.

- Heat-activate the blend: fire it in a kiln or furnace at 650 to 750 C for 1 hour. This step converts crystalline quartz into a reactive amorphous phase. Cool completely inside the kiln.

- Re-mill briefly to break up any sintered clumps.

- Dry-blend in the 5 kg of hydrated lime. Bag immediately in sealed, moisture-proof sacks.

### Field Activation

| Application | Mix Ratio (by Mass) | Cure Time |
| --- | --- | --- |
| Standard mortar or slab | 100 kg Formula 2 plus 15 to 18 liters of water, mixed to a moist crumb | 14 days |
| Extra hydraulic set | 95 kg Formula 2 plus 5 kg extra hydrated lime, plus water | 14 days |
| High-strength geopolymer | 80 kg Formula 2 (lime-free version) plus 20 kg sodium silicate solution, plus water | 7 days |

### Curing and Weather Rules

- Cast or apply the wet mix, then cover immediately with plastic sheeting or wet burlap.

- Hold the work between 20 and 40 C for the first 7 days; mist under the cover daily for the first 3 days.

- Keep rain and standing water off the work for the first 7 days; puddles leach the activator and permanently stop the reaction.

- After 14 days, the cured binder beads water, sheds rain, and resists freeze-thaw cycles.

## Formula 3: Hearthstone Slab (Improved Path C)

A permanent, weatherproof, walkable fire barrier. This version adds gypsum to the original hybrid recipe. Gypsum releases bound water vapor when fire heats it, adding an active cooling mechanism, and it accelerates the early set so the fresh slab tolerates unexpected drizzle sooner.

| Attribute | Value |
| --- | --- |
| Role | Permanent structural firebreak slab for perimeters, walkways, and utility bases |
| Cost | About $0.30 to $0.40 per kg installed |
| Lifespan | 5 to 10 or more years outdoors |
| Rain tolerance | Critical during the 7-day cure; fully waterproof and freeze-thaw resistant after 14 days |
| Wind tolerance | Total; the cured slab is a monolithic ceramic-like mass |

### Recipe (Makes 100 kg of Dry Mix)

| Component | Mass | Function |
| --- | --- | --- |
| Formula 1 aggregate (premixed 50/15/27/8) | 63 kg | Thermal insulation and structural filler |
| Formula 2 binder, heat-treated mineral fraction only | 25 kg | Reactive pozzolanic glue |
| Hydrated lime Ca(OH)2 | 7 kg | Alkaline activator |
| Gypsum CaSO4 (plaster) | 5 kg | Endothermic fire coolant; accelerates early set |
| Molasses or brown sugar | 1 kg (dissolved in the mix water) | Set retarder; extends working time to 45 minutes |
| Water | 15 to 18 liters | Added during mixing; not part of dry mass |

### Mixing and Curing Protocol

- Phase 1, dry premix: combine the Formula 1 aggregate, Formula 2 binder, lime, and gypsum. Dry-mix 7 to 10 minutes until uniform pale grey.

- Phase 2, wet activation: dissolve the molasses in 15 liters of water. Pour the solution into the dry mix while the mixer runs. Add water gradually until the mix clumps in a squeezed fist without dripping. Total water stays between 15 and 18 liters per 100 kg of dry mix.

- Phase 3, placement: place the wet mix within 45 minutes into formwork or a trench at least 10 cm thick and 2 m wide. Compact aggressively with a plate compactor or hand tamper until a faint water sheen appears. Trowel the surface smooth to close the pores.

- Phase 4, curing: cover immediately with plastic sheeting or wet burlap. Mist under the cover daily for the first 3 days. Allow foot traffic after 7 days and vehicle loads after 14 days.

### Performance Notes

- Compressive strength lands near 5 to 8 MPa, comparable to weak concrete.

- The slab withstands direct torch flame for 30 minutes with under 100 C temperature rise on the underside.

- Gypsum releases about 20% of its own mass as water vapor near 150 C, actively cooling the slab surface during flame contact.

- Wildfire exposure densifies the slab further; the surface sinters into a harder refractory skin.

## Formula 4: Skyfall Blanket (Improved Path D)

A heavy, cohesive, single-use smothering agent for aerial or ground drops directly onto a flame front. The improved version replaces part of the crusher dust with bentonite and adds gypsum. A light pre-drop misting starts the bentonite swelling, so the falling load clumps into micro-aggregates that resist wind scatter, and the landed blanket seals itself against rain and oxygen.

| Attribute | Value |
| --- | --- |
| Role | Mass-drop smothering blanket for active flame fronts |
| Cost | About $0.08 to $0.15 per kg in bulk |
| Lifespan | Single use; the fire sinters it into a glassy crust |
| Rain tolerance | High after landing; the bentonite crust self-seals and the biochar stays trapped |
| Wind tolerance during drop | High; pre-misted agglomerates fall as heavy clumps, not dust |

### Recipe (Makes 1,000 kg / 1 Metric Ton)

| Component | Mass | Share | Sieve Size |
| --- | --- | --- | --- |
| Silica tailings | 320 kg | 32% | < 2 mm |
| Granite fines | 230 kg | 23% | < 2 mm |
| Crusher dust | 150 kg | 15% | < 5 mm |
| Biochar / wood ash | 140 kg | 14% | < 2 mm, volatile matter < 3% |
| Sodium bentonite clay | 80 kg | 8% | Fine powder |
| Hydrated lime Ca(OH)2 | 50 kg | 5% | < 0.5 mm |
| Gypsum CaSO4 | 30 kg | 3% | < 0.5 mm |

Total: 100% | 1,000 kg

### Mixing and Loading Protocol

- Dry-mix all seven components for 10 to 15 minutes until uniform pale grey with dark speckles.

- During the final 3 minutes of mixing, mist in 30 to 50 liters of water (3 to 5% by mass). The bentonite begins to swell and binds the fines into micro-agglomerates of 1 to 5 mm.

- Load hoppers, Bambi buckets, or bulk bags immediately after misting. Deploy within 24 hours of misting for best cohesion.

- Drop directly onto the flame front, or 10 to 20 meters ahead of it to build a pre-emptive smothering line.

### How the Improved Blanket Works

- The heavy, pre-misted agglomerates punch through the convection column without wind scatter.

- The blanket forms a cohesive 5 to 10 cm mat over the fuel and cuts the oxygen supply.

- Gypsum releases water vapor near 150 C and lime dehydrates near 500 C; both reactions absorb heat at the flame front.

- Biochar consumes oxygen at the fuel surface as it slowly oxidizes.

- Bentonite, lime, silica, and alumina react under heat to form a calcium-aluminosilicate crust that seals the fuel bed from re-ignition.

- After the fire, rain swells the residual bentonite and locks the blanket in place as an erosion-control layer rather than washing it away.

### Application Rates

| Method | Best For | Rate |
| --- | --- | --- |
| Helicopter bucket | Spot fires, steep terrain | 1 to 3 tons per drop; covers 50 to 100 m2 |
| Fixed-wing air tanker | Large fire fronts | 5 to 20 tons per drop; covers 500 to 2,000 m2 |
| Ground hopper spreader | Pre-positioned linear breaks | Continuous feed along the line |
| Hand crew | Small fires, structure protection | 50 to 100 kg per worker; covers 5 to 10 m2 |

# 5. Part Two: Four New Formulas

Each new formula extends one of the four improved paths into a new deployment form. All four share the same ingredient family, so one stockpile feeds every product.

## Formula 5: Stonegrain Pellets (Derived from Path A)

Dense, rain-resistant granules for aerial drops and broadcast spreading. Pelletization solves the last weakness of loose mixes: dust drift during the drop and erosion before the barrier ever sees a fire. Each pellet carries the full Emberline Base chemistry inside a bentonite-and-starch shell.

| Attribute | Value |
| --- | --- |
| Role | Pelletized firebreak granules for aerial drops, steep slopes, and windy ridges |
| Cost | About $0.08 to $0.12 per kg |
| Lifespan | Two or more seasons in place; indefinite in dry storage |
| Rain tolerance | Very high; pellets swell and knit into a continuous sealed mat when wet |
| Wind tolerance | Very high; 5 to 10 mm pellets at roughly 1.8 g/cm3 fall true and stay put |

### Recipe (Makes 100 kg of Dry Feed)

| Component | Mass | Function |
| --- | --- | --- |
| Quartz tailings (fines) | 40 kg | Structure and heat sink |
| Crusher dust | 25 kg | Density and interlock |
| Biochar / wood ash | 20 kg | Insulation |
| Sodium bentonite clay | 12 kg | Wet-activated pellet binder and mat sealant |
| Cornstarch | 3 kg | Dry-strength binder; keeps pellets intact until rain arrives |
| Water | 18 to 22 liters | Pelletizing moisture; evaporates during drying |

### Production Protocol

- Dry-mix all five dry components for 10 minutes until uniform.

- Spray in the water gradually while mixing, until the blend holds together in a squeezed fist.

- Form pellets of 5 to 10 mm: roll small batches by hand on a tray, extrude through a manual pellet press, or tumble in a rotating drum or cement mixer with a spray bottle of water.

- Sun-dry the pellets for 48 hours, or oven-dry at 80 C for 4 hours, until hard and moisture-free.

- Run the drop test from Section 8: at least 85% of pellets survive a 3-meter drop onto plywood intact.

- Store in sealed bags or covered bins. Apply by air drop, broadcast spreader, or hand at 12 cm of settled depth.

### Why Pellets Beat Loose Mix for Drops

- A 5 to 10 mm pellet falls at high terminal velocity and ignores crosswinds that scatter fine powder.

- The cornstarch binder holds each pellet through handling, flight, and impact.

- The first rain dissolves the starch, the bentonite swells, and neighboring pellets weld into one continuous mat that water flows over rather than through.

- Post-fire residue degrades into a soil amendment of minerals, clay, and char.

## Formula 6: Clayshield Coating (Derived from Path B)

A sprayable mineral gel that coats structures, fences, and vegetation ahead of an approaching fire. The formula follows the USDA Agricultural Research Service finding that sodium bentonite plus starch forms a fire-protective coating that resists slumping, stays hydrated longer than commercial gels, and shields wood siding for up to 30 minutes of flame exposure. The Formula 2 mineral powder turns the dried film into a ceramic-like skin.

| Attribute | Value |
| --- | --- |
| Role | Spray-on emergency coating for buildings, fences, and fuel breaks |
| Cost | About $0.10 to $0.18 per kg of mixed slurry |
| Lifespan | Effective for days once applied; re-wet to refresh |
| Rain tolerance | High once dry; the film absorbs rain, swells, and stays adhered instead of washing off |
| Wind tolerance | Total after drying; the coating bonds to the substrate |

### Recipe (Makes About 100 Liters of Slurry)

| Component | Mass / Volume | Function |
| --- | --- | --- |
| Water | 70 liters | Carrier |
| Formula 2 mineral powder (heat-treated) | 15 kg | Ceramic-like fireproof skin after drying |
| Sodium bentonite clay | 8 kg | Gelling and moisture retention |
| Cornstarch | 2 kg | Adhesion and anti-slumping |
| Hydrated lime Ca(OH)2 | 2 kg | Mild activator; stiffens the dried film |
| Iron oxide pigment (optional) | 0.5 kg | Marks treated areas for crews and pilots |

### Mixing Protocol

- Fill the tank with 70 liters of water and start the agitator or a paddle mixer.

- Add the cornstarch and stir for 5 minutes until fully dispersed.

- Add the bentonite slowly; stir 15 minutes until the mix gels to a yogurt-like consistency.

- Add the Formula 2 powder and lime; stir 10 minutes until smooth.

- Add the optional pigment last and stir 2 minutes.

- Apply within 24 hours with a garden sprayer, fire hose eductor, or agricultural sprayer at 3 to 6 mm wet thickness.

### Field Behavior

- The wet coating clings to vertical surfaces without slumping; the starch raises yield stress.

- Under flame, the coating forms a continuous char-and-clay crust that shields the substrate and slows drying.

- Light rain on a dried coating re-hydrates the bentonite and restores full protective moisture instead of stripping the film.

- Cleanup after the fire: hose the coating off; the residue is clay, starch, and mineral ash that soils absorb without harm.

## Formula 7: Hearthpaver Tiles (Derived from Path C)

Precast, interlocking firebreak pavers made from a densified Formula 3 mix. Crews lay them like ordinary pavers to build instant permanent firebreaks along fence lines, around structures, and around utility poles. Tiles cure in a yard, stack on pallets, and deploy any time, in any weather, because rain only touches a fully cured product.

| Attribute | Value |
| --- | --- |
| Role | Modular precast firebreak for rapid permanent installation |
| Cost | About $2.50 to $3.50 per tile (30 x 30 x 5 cm, about 8 kg) |
| Lifespan | 5 to 10 or more years outdoors |
| Rain tolerance | Total after curing; deployment happens in any weather |
| Wind tolerance | Total; interlocking edges prevent displacement |

### Recipe (Makes 100 kg of Dry Mix, About 12 Tiles)

| Component | Mass | Function |
| --- | --- | --- |
| Formula 1 aggregate (premixed) | 58 kg | Thermal insulation and filler |
| Formula 2 binder, heat-treated mineral fraction only | 28 kg | Pozzolanic glue; higher dosage for tile strength |
| Hydrated lime Ca(OH)2 | 7 kg | Alkaline activator |
| Gypsum CaSO4 | 5 kg | Endothermic coolant; accelerates demolding set |
| Crusher dust, extra fines | 2 kg | Fills micro-voids for a smooth face |
| Water | 14 to 16 liters | Added during mixing |

### Casting Protocol

- Dry-mix all five dry components for 7 to 10 minutes.

- Add water gradually to a moist-crumb consistency.

- Fill 30 x 30 x 5 cm molds with interlocking edge profiles. Compact each mold with a plate compactor or vibrating table until a water sheen appears.

- Trowel the face smooth, cover with plastic, and hold at 20 to 40 C.

- Demold after 48 hours thanks to the gypsum-accelerated set. Stack the tiles under plastic or wet burlap and cure 12 more days, misting daily for the first 3 days.

- Palletize and store indefinitely. Deploy by laying tiles on leveled, compacted soil; sweep dry crusher dust into the joints to lock the field.

### Deployment Patterns

- Perimeter ring: two tile courses (60 cm) around sheds, tanks, and structures.

- Fence line ribbon: single course along property lines to stop grass fire creep.

- Utility collar: four tiles around each pole base to block ground fires.

- Trail edge: stepping-stone lines across known fire corridors.

## Formula 8: Deepseal Grout (Derived from Path D)

A pumpable mineral grout for smoldering ground fires in peat, duff, and coal-seam-type fuels, the fire type that loose blankets and surface drops fail to reach. The grout flows into the smoldering zone, the bentonite swells to seal oxygen pathways, and optional dry ice pellets deliver deep cooling and CO2 oxygen displacement. Every component remains a common soil or food-adjacent material.

| Attribute | Value |
| --- | --- |
| Role | Injectable sealant for underground smoldering fires |
| Cost | About $0.12 to $0.20 per kg of mixed grout (dry ice extra) |
| Lifespan | Permanent seal once placed |
| Rain tolerance | Irrelevant after placement underground; surface gear works in any weather |
| Wind tolerance | Total; pumped or poured, never dropped |

### Recipe (Makes About 100 Liters of Grout)

| Component | Mass / Volume | Function |
| --- | --- | --- |
| Water | 55 liters | Carrier |
| Formula 4 mineral fines (silica, granite, crusher dust, biochar fractions) | 20 kg | Bulk, heat sink, and crust formation |
| Sodium bentonite clay | 12 kg | Swells to seal oxygen pathways in the fuel bed |
| Gypsum CaSO4 | 4 kg | Endothermic cooling inside the smoldering zone |
| Hydrated lime Ca(OH)2 | 4 kg | Sets the crust and neutralizes acidic fire residues |
| Dry ice pellets (optional) | 2 to 5 kg, added at the pour point | Deep cooling and CO2 oxygen displacement |

### Mixing and Injection Protocol

- Mix the water and bentonite first; agitate 15 minutes to a smooth gel.

- Add the Formula 4 mineral fines, gypsum, and lime; agitate 10 minutes to a pumpable slurry like thin cement grout.

- Deliver through a lance, trench pour, or injection probe into the smoldering zone at 20 to 40 liters per square meter of fire ground.

- For deep or stubborn smolder, feed dry ice pellets into the grout stream at the nozzle. The pellets ride the flow downward, then sublimate: intense cooling plus CO2 displacement of oxygen.

- Monitor surface temperature for 48 hours; re-inject any spot that regains heat.

### Why This Works Where Blankets Fail

- Peat and duff fires smolder below the surface; dropped blankets never touch them. Grout flows to the heat source.

- Hydrated bentonite forms an impermeable seal that blocks the slow oxygen seepage that feeds smoldering.

- Gypsum and free water cool the zone; dry ice adds a deep cold sink and floods the voids with CO2.

- The cured grout stays in the soil as an inert mineral fill; no cleanup follows.

# 6. Master Comparison Table

| Formula | Origin | Form | Rain Tolerance | Wind Tolerance | Cost per kg | Lifespan |
| --- | --- | --- | --- | --- | --- | --- |
| 1. Emberline Base | Path A | Loose ground barrier | High (self-sealing crust) | High | $0.06-0.10 | 1-2 seasons |
| 2. Ashbinder Powder | Path B | Dry binder powder | Waterproof after cure | N/A (solid after cure) | $0.15-0.20 | Permanent |
| 3. Hearthstone Slab | Path C | Cast-in-place slab | Waterproof after cure | Total | $0.30-0.40 | 5-10+ years |
| 4. Skyfall Blanket | Path D | Mass-drop blanket | High after landing | High during drop | $0.08-0.15 | Single use |
| 5. Stonegrain Pellets | Path A | Pelletized granules | Very high | Very high | $0.08-0.12 | 2+ seasons |
| 6. Clayshield Coating | Path B | Spray-on gel | High once dry | Total once dry | $0.10-0.18 | Days, re-wettable |
| 7. Hearthpaver Tiles | Path C | Precast pavers | Total after cure | Total | $0.30-0.40 | 5-10+ years |
| 8. Deepseal Grout | Path D | Injectable grout | N/A (underground) | Total | $0.12-0.20 | Permanent |

Table 2: All eight formulas at a glance.

# 7. Environmental Safety Verification

Every formula passes three checks: natural or waste-derived origin, no persistent toxic residue, and neutral or beneficial post-fire soil impact. The table below records the verification result for each ingredient and each deliberate exclusion.

### 7.1 Included Ingredients

| Ingredient | Verification Result |
| --- | --- |
| Quartz tailings | Inert silica; chemically identical to natural sand. Diverts mine waste from containment. |
| Granite fines | Inert crushed rock; matches native soil minerals. Diverts quarry waste. |
| Crusher dust | Inert angular rock fines; identical to road base material. |
| Biochar / wood ash | Recognized soil amendment; adds potassium and stable carbon to soil after the fire. |
| Sodium bentonite | Natural clay approved for pond liners, drilling, and food contact; swells and stays put. |
| Hydrated lime | Standard agricultural amendment; carbonates back to inert limestone within months. |
| Gypsum | Natural mineral and agricultural soil conditioner; adds calcium and sulfur plants use. |
| Cornstarch | Food product; biodegrades completely within weeks. |
| Molasses / brown sugar | Food product; biodegrades completely. |
| Sodium silicate (optional) | Cures to inert silica gel; wet solution needs gloves but leaves no toxic residue. |
| Dry ice (optional) | Sublimates to atmospheric CO2; zero residue. |
| Iron oxide pigment (optional) | Natural rust pigment; soils already contain it. |

### 7.2 Deliberate Exclusions

| Excluded Material | Reason for Exclusion |
| --- | --- |
| Ammonium phosphate retardants | Documented aquatic toxicity and algae-bloom risk when drops reach waterways. |
| Borate compounds | Documented soil toxicity; abandoned by the retardant industry decades ago. |
| PFAS and fluorinated surfactants | Persistent forever chemicals; banned from modern wildfire products. |
| Coal fly ash | Potential heavy-metal content (cadmium, chromium); biomass wood ash replaces it. |
| Sodium carbonate accelerators | Catalyzes extra volatile organic compound release during pyrolysis. |
| Synthetic superabsorbent polymers | Persistent microplastic residue in soil; starch and bentonite replace them. |
| Portland cement | High embodied CO2 from 1450 C kilns; the Formula 2 geopolymer pathway replaces it. |

Waterway Precaution

Even benign mineral drops belong outside waterways. Follow the standard 300-foot (about 90 m) buffer around streams, ponds, and riparian zones for all aerial applications of Formulas 4, 5, and 6.

The bentonite and lime in these formulas raise local pH briefly after landing. Vegetation recovers; the minerals carbonate and neutralize within one wet season.

# 8. Testing and Quality Control Protocols

Run these field tests on every new batch of raw material and every new mix. None of the tests needs a laboratory.

### 8.1 Torch Test (All Formulas)

- Spread a 500 g sample in a metal tray.

- Hold a propane torch flame to the sample for 10 seconds.

- Remove the flame. A passing sample shows no sustained glowing and releases no smoke. A failing sample glows or smokes; re-burn the biochar feedstock to full ash and test again.

### 8.2 Loss-on-Ignition Check (Biochar Quality)

- Weigh 100 g of dried biochar or ash.

- Heat it in a muffle furnace or sealed metal tin over a strong fire at about 550 C for 2 hours.

- Weigh again. Mass loss above 3% signals residual volatile matter; the batch fails and the feedstock needs a longer, hotter burn.

### 8.3 Rain Simulation (Formulas 1, 4, and 5)

- Lay a 1 m2 test plot at the design thickness, or fill a shallow tray for pellets.

- Apply 60 mm of water over 2 hours with a sprinkler, simulating a heavy storm.

- Dry the plot for 24 hours, then collect and weigh the material. Mass retention above 90% passes. Re-run the torch test on the rained sample to confirm fire performance.

### 8.4 Wind Test (Formulas 1, 4, and 5)

- Point a leaf blower or fan at the test plot from 2 meters at full power for 5 minutes.

- Weigh the plot before and after. Mass loss below 5% passes.

### 8.5 Pellet Drop Test (Formula 5)

- Drop 1 kg of dried pellets from 3 meters onto a plywood sheet.

- Count intact pellets. At least 85% intact passes. Crumbling pellets need 2 kg more bentonite per 100 kg and a longer cure.

### 8.6 Slump Test (Formula 6)

- Spray a 6 mm wet coat onto a vertical plywood board.

- Wait 10 minutes. Slumping below 10 mm of downward travel passes. Thicker runs need 1 kg more starch per 100 liters.

### 8.7 Cure Strength Check (Formulas 3 and 7)

- Cast a small puck or spare tile alongside the main work.

- After 14 days, strike the sample edge with a hammer. A passing sample chips rather than crumbles and rings solid. A crumbly sample signals leached activator; review the curing cover practice.

# 9. Field Deployment Guide

| Scenario | Recommended Formula | Notes |
| --- | --- | --- |
| Grassfire approaching within hours | Formula 1 (ground) or 4 (air) | Lay 12 cm thick, 2 m wide; drop blankets ahead of the front |
| Home or structure defense | Formula 6 now, Formula 3 or 7 for permanence | Spray siding and fences; build a slab or tile ring after the season |
| Windy ridge or steep slope | Formula 5 | Pellets stay put where loose mix scatters |
| Utility poles and fence lines | Formula 7 | Install once; maintain nothing for years |
| Smoldering peat or duff fire | Formula 8 | Inject grout; add dry ice for deep seats |
| Large fire front, air tanker available | Formula 4 | Mist the load before the drop for cohesion |
| Pre-season preparation | Formulas 3 and 7 | Install permanent works during the cool, wet months |

### General Rules for Every Deployment

- Torch-test every batch before deployment.

- Clear leaf litter and needles from any surface before laying material.

- Keep aerial drops at least 90 m from waterways.

- Record batch ratios, weather, and test results for every deployment; the record drives continuous improvement.

# 10. Bulk Sourcing Guide

| Material | Cheapest Bulk Source | Typical Cost |
| --- | --- | --- |
| Quartz tailings | Quarries, sand mines, glass-sand processors; often free for hauling | $0 to $10 per ton |
| Granite fines | Dimension-stone and aggregate quarries; ask for crusher screenings | $0 to $15 per ton |
| Crusher dust | Any rock quarry or gravel pit; the sweepings under the crusher | $0 to $10 per ton |
| Biochar / wood ash | Sawmills and wood shops; burn residue fully in a controlled pit to white ash | Labor only |
| Sodium bentonite | Drilling-mud suppliers, pottery suppliers, or plain clay cat litter (100% bentonite, fragrance-free) | $5 to $15 per 25 kg |
| Hydrated lime | Agricultural co-ops and builders merchants | $8 to $15 per 25 kg |
| Gypsum | Hardware stores (plaster) or agricultural gypsum sacks | $10 to $20 per 25 kg |
| Cornstarch | Restaurant or bakery bulk suppliers | $20 to $40 per 25 kg |
| Molasses | Feed stores (stock-feed molasses) | $15 to $30 per 20 liters |
| Sodium silicate (optional) | Chemical suppliers or concrete-admixture dealers | $1 to $2 per kg |
| Dry ice (optional) | Industrial gas suppliers and food cold-chain depots | $1 to $3 per kg |
| Iron oxide pigment (optional) | Concrete-coloring suppliers | $2 to $5 per kg |

Table 3: Prices reflect typical 2025-era bulk rates and vary by region; quarry waste often costs only the hauling.

# 11. Naming Convention

Each formula carries a descriptive, politically neutral name drawn only from the material, form, or function of the product. No name references any nation, movement, ideology, or person, so the system travels anywhere without friction.

| Formula | Name | Name Origin |
| --- | --- | --- |
| 1 | Emberline Base | A ground line that stops embers |
| 2 | Ashbinder Powder | A volcanic-ash-analogue binder |
| 3 | Hearthstone Slab | A stone slab that guards the hearth |
| 4 | Skyfall Blanket | A blanket that falls from the sky |
| 5 | Stonegrain Pellets | Stone formed into grains |
| 6 | Clayshield Coating | A clay shield sprayed as a coating |
| 7 | Hearthpaver Tiles | Pavers that protect the hearth |
| 8 | Deepseal Grout | A grout that seals deep ground fires |

End of v1.0: test every batch, record every deployment, and improve the next version from field data.